Beam Into Undulator Protection Collimator

J. C. Sheppard, June 11, 2004

EGS code: 	~/egsruns/yieldcalc/phtnspctrm/temp/Edepo.mortran

~/egsruns/yieldcalc/phtnspctrm/temp/wpc.data

~/egsruns/yieldcalc/phtnspctrm/temp/wpch.data

50 GeV electrons into W cylinder

Beam centered on front face of collimator without hole. Use EGS to estimate absorption in collimator and peak energy deposition. Incident beam has 40 m rms transverse spot size. Number of incident electrons: 100

| Diameter (cm) | Length (cm) | Absorption (%) |
| --- | --- | --- |
| 6 | 10 | 97.8 |
| 8 | 10 | 98.9 |
| 10 | 10 | 99.2 |

Peak energy absorption in collimator: 1x1010 @ 50 GeV = 80 J/pulse,= 19.3 g/cm3

| Z1 | Z2 | E/E/vol (max) | E/mass (max) | T (peak) |
| --- | --- | --- | --- | --- |
| r.l. | r.l. | Fraction/cm3 | J/g | oC |
| 0 | 1 | 8.5 | 35 | 263 |
| 1 | 2 | 26 | 108 | 805 |
| 2 | 3 | 54 | 224 | 1672 |
| 3 | 4 | 68 | 282 | 2105 |
| 4 | 5 | 66 | 274 | 2043 |
| 5 | 6 | 58 | 240 | 1796 |
| 6 | 7 | 45 | 187 | 1393 |

Absorption of pencil beam as a function of incident distance from edge of 0.75 mm hole

Use 25, 50 GeV incident electrons; 6 cm diameter cylinder

| r (microns) | r (microns) | Absorption (%) |
| --- | --- | --- |
| 376 | 1 | 97.4 |
| 380 | 5 | 97.3 |
| 400 | 25 | 97.4 |
| 500 | 125 | 97.8 |
| 625 | 250 | 97.8 |